## Slide 1: Investigation of Hall Effect Thruster Channel Wall Erosion Mechanisms
Aaron M. Schinder
Advisor: Prof Mitchell Walker
Advisor: Prof Julian Rimoli
Georgia Institute of Technology
Montgomery Knight 317
2 August 2016

## Slide 2: Outline
Introduction and Motivation
Background on Erosion Research and Modeling
Research Contributions/Goals
  3D Raytracing Model of Heterogeneous Plasma Erosion
  Thermo-Mechanical Model of Multi-kW HET
  Investigation of Strain Relief Hypothesis
  Stressed Erosion Experiment
  Results of Stressed Erosion Exposures
  Model for Development of Cell Pattern
  Discussion of M26 Evolution
Summary
Conclusions

## Slide 3: Introduction
Types of Rocket Propulsion:
Chemical Propulsion
  Can be high thrust (10s kN)
  Isp less than 450s specific impulse
  Impulsive maneuvers
Electric Propulsion
  Low thrust (mN – 100s mN)
  Isps can be arbitrarily high (2000-4000 sec typical)
  Low-thrust constant acceleration maneuvering
Chemical
Electric
Notes: With a few limited exceptions, maneuvering in space requires expending propellant to accelerate. Spacecraft maneuverability is governed by the rocket equation, relating the delta-V of a given maneuver to specific impulse to give the mass fraction the vehicle must expend as propellant.
Rockets can be broadly divided according to where they get the energy to accelerate the propellant. Chemical propulsion uses a chemical reaction of the propellant to accelerate the jet. Power can be very large, as can thrust, but Isp is limited by the specific energy of the chemical reaction.
Electric propulsion uses an external power source to accelerate the jet. Electric propulsion tends to be lower power, and lower thrust, but there is no limit to the specific energy, and hence Isp, that can be applied to the jet. EP tends to be more mass efficient. Acceleration must be done over periods that are long relative to orbit timescales, leading to more complicated maneuvering.

## Slide 4: Introduction
Hall Effect Thrusters (HETs)
  Electrostatic propulsion device
  Isps between 1300 and 3000 sec
  Can operate at high thrust-to-power
Operation of HET
  Magnetic field traps electrons near exit plane
  Energetic electrons ionize neutral gas
  Electric field between anode and electrons accelerates ions
Diagram of HET Operation
Notes: Hall Effect Thrusters are a type of electrostatic propulsion device. Electrostatic refers to the acceleration of ions by a static electric field. They are a promising device because of their ability to operate at high thrust-to-power relative to gridded ion engines, and their avoidance of space-charge limits on thrust per area.
HETs operate by trapping a cloud of electrons, emitted by an external cathode, in an annular region near the exit plane of the dischrage channel. The electrons are energized by the crossed electric and magnetic fields. They ionize neutral gas injected in the upstream end of the channel, producing ions which see the electric field and accelerate. The cathode also neutralizes the resulting propellant jet. Key components of the thruster are the cathode, anode gas-distributor, magnetic circuit which traps the electrons, and the ceramic discharge channel wall, which protects the magnetic circuit from energetic ion bombardment.

## Slide 5: Background
Life Limiting Mechanisms for HETS:
  HETs can fail suddenly
    Thermal Shock
    Cathode Failure
  Properly designed HETs fail gradually
    Ceramic (boron nitride or borosil) shields magnetic circuit, is eroded over time
    Ions are created in last 1-2cm of channel
    Ions are accelerated, E>50 eV -> sputtering of wall material
Erosion process in a HET discharge channel

## Slide 6: Motivation
Models exist for average erosion, but:
Unexplained features:
  Composition changes [1,2]
  Microstructural roughening of borosil composites [4]
  Anomalous Erosion Ridges developed during long duration life testing [5]. First seen during M100 testing.
  In order to develop reliable predictive models, explanations for these features must be found.
BPT-4000 anomalous erosion ridges after 10,400 hours of exposure [3].

## Slide 7: Motivation
Can we predict these features (research question)?
SPT-100 after 5730-hr qualification life test
PPS-1350G after 2600-hr qualification life test

## Slide 8: Background on Erosion Research and Modeling
2 General Approaches to Estimating Thruster Life:
1. Direct empirical testing [Peterson and Manzella]:
  Run a test thruster for 100 hours and measure the channel walls to derive erosion rate.
  Strength: Experimental. No ambiguity about model fidelity.
  Weakness: Cannot assume a constant erosion rate. Erosion rate slows down over time.
2. Plasma Models coupled with Material Yield Model
  Plasma model (2D axisymmetric) models plasma in channel
    Gives ion impact rates
    Ion impact energies
  Material yield model used to update wall geometry.

## Slide 9: Background on Erosion Research and Modeling
Research on plasma erosion has focused on the following areas:
  Atomic sputtering yield models: Data from ion beam exposure experiments. Theoretical models curve-fit to data. Sparse data below 250 eV.
  Computational modeling: Yim’s molecular dynamics of h-BN sputtering [6].
Yim’s MD simulation domain after ion impacts. Adapted from [6].
Empirical sputtering yield data and curve fits [7,8].
Atomic sputtering: Incident ion,
low avg # of atoms removed (0-5)
Boron
Nitrogen
13 nm
Notes: Maybe remove this slide, maybe make it a backup slide
2 approaches to yield data
Experiment
Molecular dynamics modeling

## Slide 10: Background on Erosion Research and Modeling
Computational Erosion Modeling:
  Joins a plasma model (usually 2D axisymmetric simulation such as HPHall) to a sputtering yield model.
  Calculates ion impact energies/rates
  Updates wall geometry.
Limitations of Present Modeling:
  Many free parameters
  Models are 2D – no way to model azimuthal patterns such as anomalous erosion ridges
  Material is treated as homogeneous and isotropic with simple yield behavior
SPT-100 inner channel wall, Gamero-Castano’s computations vs. experimental data [7].
Notes: Match nomeclature: Computational models vs plasma models

## Slide 11: Research Goals
The goals of this research are to explain currently unexplained features:
The effect of plasma erosion on a complex heterogeneous material.
  The effects of material heterogeneity on the generation of surface features.
  The effects of ion impact angles on the generation of surface features.
The process by which large 3D structures, such as the anomalous erosion ridges grow.
Notes: Frame my problems
I want to be able to explain:
  Effect of material inhomogenieties
  Effects of 3d structures of materials

## Slide 12: 3D Raytracing Model of Heterogeneous Plasma Erosion
AFRL/UM P5 thruster investigated with SEM microscopy and XPS profilometry [4].
M26 Borosil Material:
  Complex heterogeneous composite
  Thin (0.1 x 10-100 µm) BN flakes
  Silica matrix
Plasma erosion of a complex material is more complex than simple heterogeneous model.
AFRL/UM P5 Outer Channel
SEM of M26 Material Cross Section
Investigation, model and results published in JPP paper:
A. Schinder, M. Walker, and J. Rimoli, “3D Model for Erosion of a Hall Effect Thruster Discharge Channel Wall,” Journal of Propulsion and Power, vol. 30, no. 5, pp. 1373–1382, 2014.
Notes: The eroded channel wall of the AFRL/UM P5 thruster was sectioned and investigated with SEM microscopy and XPS spectroscopy to show details of the material, surface features, and composition. SEM imaging reveals that M26 borosil, a common material used in many HETs, is a complex heterogeneous material composed of thin BN flakes in a silica matrix.
The evolution of this material under plasma erosion is very complex. Hilly “cliff-and-valley” surface features are observed in the HE region. In addition, a change in the composition of the HE region is seen relative to the 60% BN/40% SiO2 composition seen in the non-eroded region.
A model was created to help us understand how plasma erosion of this material proceeds.

## Slide 13: 3D Raytracing Model of Heterogeneous Plasma Erosion
3D Raytracing Model Created to Understand Evolution of Borosil [4]:
  3D model of material domain. Grains and matrix.
  Models ions with a given energy and impact angle.
  Models surface geometry and shadowing.
  Sputtering models for each exposed material.
Notes: (emphasize no one has created a 3d model of borosil erosion yet)
Talk about assumptions: atomic sputtering, erosion local to the surface
A model was created to understand how plasma erosion of borosil develops. This model is composed of a 3D model of the material – the distribution of grains and matrix within the material. It models the development of an initially flat surface profile as ions impact the surface at a given ion impact energy and impact angle. The local erosion rate, at each node is calculated for the exposed material at that node. Whether or not the node is in shadow, protected from the ion beams; or if it is exposed is calculated at each timestep. The surface geometry is updated, and the surface is propagated into the material domain.
This model produces surface geometry, and surface composition for complex heterogeneous materials, assuming simple atomic sputtering on the level of the individual material grains.

## Slide 14: 3D Raytracing Model of Heterogeneous Plasma Erosion
Model successfully reproduces observed features:
  Streak-marks at smallest scale
  The development of “pike-tongue” features [references].
  RMS roughness of 6 ± 2.5 µm observed, 8 µm predicted for 30° incidence angle.
  Have not yet captured macro-scale features (anomalous erosion ridges).
a) Simulated erosion surface, b) SEM image of highly eroded section of channel wall.
Notes: Put reference to journal article that I published
Put in color images
Blow up RHS image
Show cliff and valley image earlier, (slide 14)
Then we explain it
Two different models of the exposed material were created. One at the smallest scale reproduced the 10 micrometer scale streak marks observed in SEM imaging at high magnification.
Shown here are the cliff-and-valley structures, which, in the model, appear as a consequence of BN rich clusters protruding from the surface of the material, and shielding the softer, higher yield silica behind the protrusions from ions at a shallow incidence angle to the surface.
Ions at shallow incidence angles of 30 degrees also reproduced the observed RMS roughness. Microscopy of the HE region gave RMS roughness estimates of 6 micrometers. The simulation reproduced about 8 micrometers for large erosion depths and 30 degrees incidence to the surface plane.

## Slide 15: Can this Model Explain the Anomalous Ridges?
The behavior of the 3D erosion model tends to asymptote with erosion depth.
No new features after a few multiples of the grain lengthscale.
Need a different explanation.
RMS roughness and peak-to-valley depth as a function of average erosion depth, 30º ion incidence.
Notes: Maybe put a picture of the ridges.
Describe model

## Slide 16
We also want to understand anomalous ridges:
Pure atomic sputtering and heterogeneity may not be able to explain anomalous ridges:
  The development of surface features appears to reach steady state
  Length-scales seem governed by material grain sizes and ion impact angle
Other plasma phenomena:
  Plasma sheath: Debye lengthscale in HET channel wall is on the order of xx um – too small
  Electron gyroradius – On the same order as [Morozov]
  Ion cyclotron drift instability: 0.1-0.4 mm in azimuthal direction in HETs [Katz]
One neglected source of energy and potential instability:
  HET channel walls are under thermo-mechanical stress.
Notes: Ira Katz has a paper on a wave instability that he thinks can match up to these ridges.

## Slide 17: Thermo-Mechanical Modeling of Multi-kW HET
To figure out if the stress is interesting need to know: What sort of stresses are present in HETs.
Thermography studies:
  Martinez [9]: Thermocouples on T-140.
  Mazouffre [10]: Infrared camera images of PPSX000 and SPT-100.
  Polk – 2 temperature IR camera in H6
Model of T-140 channel wall created.
  Boundary conditions from T-140 channel thermal environment and mechanical support.
  Heat flux in high electron-temp region of thruster plasma.
  Reproduce experimental temperature distributions.
Thermo-mechanical model boundary conditions for T-140
Notes: Reference Polk paper?
Spektor Aerospace Corporation paper?
Maybe put reference thermo-mechanical image
One of the main questions tested in our research is whether or not thermo-mechanical stress has an effect on plasma erosion. One hypothesis that is investigated is that the presence of stress could lead to unstable waves in a material surface profile during erosion, and possibly to the anomalous erosion ridges.
In order to understand the stresses that will be present in the channel wall material, it is necessary to model the thermo-mechanical stresses implied by reasonable temperatures in Hall Effect Thrusters. A 2D thermo-mechanical model of the T-140 channel wall is created. In this model, the majority of the heat flux is expected to be in a thin region near the exit plane, where the electron temperature and plasma density peaks for a HET. According to plasma-wall interaction physics, investigated by Goebel and Katz, and Hobbes and Wesson, the heat loading to an insulating wall is a function of the ion and electron flux to the wall, which is mediated by the plasma sheath. The salient point for this model is that the majority of the power loss to the wall takes place in the region of highest plasma density. The inner faces of the channel are assumed to radiate to free space. These assumptions tend to reproduce experimentally observed temperature variations across the T-140 channel wall.
The channel is held mechanically to the thruster by rivets or pins at the bottom of a titanium radiation-shielding bucket. These pins allow for loose mechanical boundary conditions. The thermo-mechanical stress appears in the model as the result of temperature gradients in the thruster itself.

## Slide 18: Thermo-Mechanical Modeling of Multi-kW HET
Power loss to the wall:
  Assumed to be 25-27% of the discharge power.
  Reproduces Martinez’s average temperature measurements in both 2D model and simple radiative equilibrium model.
Average channel wall temperature vs. discharge power for simple radiative balance model, 2D thermo-mechanical model, and Martinez’s data [9].
Notes: Power deposition to the channel wall has historically been a stable percentage of the discharge power at which the thruster operates. In this thermo-mechanical modeling, the percentage of the discharge power applied to the channel wall is chosen so that the temperatures and temperature distributions produced by the model match those observed experimentally for various operating conditions. In addition, the average heat flux to the wall should match those predicted by plasma physics (5-10 W/cm2). (10 W/cm2 calculated for 3400 W operating condition)

## Slide 19: Expected/Predicted Stress Range
Between 100 kPa (HP BN) and 6 MPa compressive hoop stress (highest power, M26 borosil) is expected for the T-140. Stresses in this range are thought to be typical for multi-kW class HETs.
Wall Material | Discharge Power | Outer Thermal BC | Max Temperature | Max Compressive Hoop Stress
(grade) | (W) |  | (K) | (MPa)
M26 | 840 | Insulated | 605 | -1.89
M26 | 2000 | Insulated | 779 | -3.82
M26 | 2800 | Insulated | 862 | -4.93
M26 | 3400 | Insulated | 913 | -5.69
HP | 840 | Insulated | 576 | -0.15
HP | 3400 | Insulated | 808 | -0.44
M26 | 840 | Radiating | 564 | -2.06
M26 | 3400 | Radiating | 873 | -6.14
HP | 840 | Insulated | 576 | -0.15
HP | 1500 | Insulated | 674 | -0.26
HP | 2000 | Insulated | 732 | -0.33
HP | 2400 | Insulated | 807 | -0.44
HP | 3400 | Insulated | 855 | -0.52
Notes: Need a takeaway on the bottom of the slides.
Two channel wall materials and a variety of power conditions were investigated. Grade HP boron nitride has lower thermal expansion and elastic modulus, and much higher thermal conductivity than the M26 borosil material, and so has about 10x less thermo-mechanical stress predicted. The range of stresses estimated by the model are between 100 kPa and 6 Mpa. It is not physically realistic to expect more than 30 Mpa to be present in a properly designed HET (with appropriate mechanical boundary conditions) because that exceeds the flexural strength of the material and would lead to cracking of the channel.

## Slide 20: IS Mechanical Strain Energy Important?
If we assume:
  The dominant mechanism for removing material is purely atomic sputtering
  The cost of removing material is dominated by the cost of atomic sputtering
  Strain energy density is an average linear-elastic quantity without grain-mediated stress concentrations
Then:
  Strain energy densities are orders of magnitude smaller than thermal energy, atomic bond energy, sputtering energy densities
  Predicted timescales of the growth of perturbations are on the order of 108 hrs or more.
However: If we relax these assumptions:
  Strain energy densities / Free surface energy  Potential instability with λ in mm ranges.
Property | Value | Unit
B-N Covalent Bond Energy | 3.9 | eV/bond
Thermal Energy of HP BN at 1000K | 0.1 | eV/atom
Average elastic strain energy of HP BN at 45 MPa average load. | 1.6×10-6 | eV/atom
Threshold energy below which no appreciable atomic sputtering is detectable. | 18 | eV/ion
Ion energies in HETs | 200-400 | eV/ion
Energy scales of atomic sputtering, thermal, and mechanical strain energy
Notes: If I use one set of assumptions about what material properties are, this might not be interesting.
If we break these, however, there could be a surface instability present which may make this stress range important in production of features with a given wavelength range

## Slide 21: Investigation of Strain Relief Hypothesis
Strain Relief Hypothesis:
  Prompted by acid-etching instability studied by Kim, Hurtado, and Tan [11], and analogies with stress-corrosion-cracking.
  Presence of elastic strain energy in material drives instability.
  Variations in surface height  Variations in strain energy near surface  Generalized forces amplifying variations.
M – kinetic constant of the process
γ – Free surface energy
h – variation to surface height
Δw – variation in strain energy density
σ0 - average stress in material
Cross section of problem domain showing variations to strain energy due to variations in average surface profile.
Notes: Have a backup slide about assumptions behind M
A hypothesis is investigated which was proposed to explain the anomalous erosion ridges in Hall Effect Thrusters. The strain relief hypothesis proposes that variations to the profile of the surface of a material can lead to variations in the strain energy denstiy in a material under an average stress. These variations in strain energy density near the surface lead to generalized forces which act on a process doing work (eroding) the surface. This instability is driven by the release of the mechanical strain energy, and opposed by the surface energy.
Kim, Hurtado, and Tan studied this phenomenon as it relates to acid etching of Aluminum. In their work, aluminum samples were placed under plastic deformation, at stresses of 200 Mpa, and etched with nitric acid. Atomic force microscopy of the surfaces showed that certain wave-modes of variation to the surface are amplified over time.

## Slide 22: Investigation of Strain Relief Hypothesis
Strain Relief Hypothesis:
  Variations in surface profile produce variations in strain energy density
  Changes in h(x) give rise to generalized forces due to changing Δw and surface energy.
  Predicted: Range of unstable wavelengths [0, ωcr] which grow in time.
Nomenclature:
Avg Height: H(t)
Variational Height: h(x,y,t)
Macroscopic Stress: σ0
Variational Strain Energy Density Δw
Amplification Function Ψ
Critical Wavenumber ωcr
Material elastic properties: μ, ν
Material free surface energy: γ
Stress State: σ, σp
Kinetic Constant of the Erosion Process: M
Ψ
ω, or ν
ωcr
ωmg
growth
damping
Wavelength scale a function
of mechanical stress state.

## Slide 23: Wavelengths of Unstable Modes
Predicted spatial frequency of maximum growth as a function of material stress for borosil material:
Range of Predicted Stresses
Flexural
Strength
Limit
Range of viability
Notes: Show what we predicted
Show material limits on slide

## Slide 24: Stressed Erosion Experiment
Does the presence of mechanical stress affect plasma erosion of materials?
Experiment designed to answer this question:
Pairs of samples exposed to argon plasma for 11-12 hrs:
  Test conducted in GTRI’s Ion Assisted Deposition (IAD) chamber
  One sample loaded to up to 25 MPa: Experiment sample
  One sample free to expand: Control sample
Material Selection:
  Fused silica samples: Amorphous, isotropic. No microstructural detail: Can study the erosion of a surface without variations due to material medium.
  M26 borosil: A complex composite material. Borosil is used in many HETs. Strong perturbations from material heterogeneity expected.
  3x1x0.25 in samples, pre-roughened to provide seed for surface growth.
Test Fixture
Plasma Source
Beam Core
Samples
25cm
32 cm
4cm
Beam Window

## Slide 26: Stressed Erosion Experiment
Test fixture design:
  Moment free compressive load applied to sample.
  Belleville spring-stack maintains mechanical load during thermal expansion of clamp.
  Characterized relaxation vs. temperature with a series of digital image correlation experiments
    Measured thermal expansion of all components
    Measured changes in stiffness as a fn of stress for spring stack
    Calculate relaxation vs. temperature
  Thermocouple measures clamp temperature during test.

## Slide 27: Stressed Erosion Experiment
Test fixture and instrumentation
Plasma
Preheater Pads
Experiment Sample
Control Sample
Strain Gages
Plasma Source
Thermocouple
16 cm

## Slide 28: Stressed Erosion Experiment
Test Phases:
  Pre-Exposure:
    Line-scans: Provide pre-exposure fourier statistics. 50 scans with Tencor P-15 contact profilometer.
    Microscopy: Olympus LEXT
  Exposure:
    Sample pair placed in test fixture.
    Loaded to desired load.
    Exposed for period of 12 hours.
  Post-Exposure:
    Line-scans
    Microscopy: Revisit same areas
Ψ
ω, or ν
ωcr
ωmg
Pre and post-test linescans -> Ψ

## Slide 29: Results of Stressed Erosion Experiment
Fused silica exposures: Four exposures
  3 Exposures: Pre-roughened samples
  Series of 3 increasing load levels
  One exposure with smooth samples (+/- 0.05 µm)
M26 exposures:
  Two exposures at two load levels
Exposure | Fused Silica 1 | Fused Silica 2 | Fused Silica 3 | Fused Silica 4 | M26 1 | M26 2
Loaded Sample | SA7 | SA1 | SA8 | SA6 | SC1 | SC4
Control Sample | SA4 | SA5 | SA9 | SA10 | SC3 | SC5
Initial Stress State (MPa) | 9.6 | 17.5 | 18.1 | 29.1 | 23.4 ± 3.1 | 27.2 ± 3.7
Equilibrium Temp (C ) | 288 ± 12 | 225 ± 8 | 224 ± 5 | 243 ± 5 | 241.3 ± 15.6 | 258.6 ± 2.4
Relaxed Stress State (MPa) | 6.00 ± 1.01 | 14.36 ± 1.01 | 14.94 ± 0.97 | 24.99 ± 1.10 | 20.6 ± 3.3 | 24.1 ± 3.4
Relaxed Stress State (% orig.) | 62.5 ± 10.5 | 82.05 ± 5.79 | 82.57 ± 5.36 | 85.87 ±3.79 | 77.6 ± 12.3 | 77.8 ± 1.1
Duration (hrs) | 11 | 11 | 11 | 11 | 12 | 12
Pre-Roughened | Yes | Yes | No | Yes | Yes | Yes
Exposure Overview

## Slide 30: Results of Stressed Erosion Experiment
Fused silica amplification functions:
  Pre an post-test profilometry statistics provide Ψ
  Region of growth for λ> 0.1 mm
  No difference observed between series ΔΨ<0.15, <0.05 for sample pairs
  No apparent dependence on applied load

## Slide 31: Results of Stressed Erosion Experiment
Development of cusped-cell pattern:

## Slide 32
Cell pattern develops where initial surface features are present:
Notes: Initially smooth samples remain smooth. Initially rough areas develop cell pattern.

## Slide 33: Results of Stressed Erosion Experiment
M26 pre and post-exposure surface statistics:
  Final surface statistics are insensitive to initial surface roughness.
  All post-test statistics similar to within 0.01 µm/wavemode.

## Slide 34: Results of Stressed Erosion Experiment
Pre and post-exposure microscopy:
  Boron nitride flakes, and BN rich areas protrude from silica matrix
SC1 100x magnification post-exposure a) visible light image, b) laser height map.
Shows BN rich regions protruding from the silica material.

## Slide 35: Model for Development of Fused Silica Cell Pattern
1D angle dependent model for fused silica evolution:
  Local normal to surface
  Takes variation in sputtering yield with incidence angle into account
  Reproduces development of cusped cell pattern qualitatively and quantitatively
Sputtering yield as a function of ion incidence angle. Data from [8].
Blue: Line-scan profiles from fused silica surface.
Black: Simulated propagation of pre-test surface according to model.

## Slide 36: Discussion of Fused Silica and M26 Evolution
Evolution of fused silica is governed by:
  Initial surface structure (post test statistics are proportional to pre-test statistics).
  Angle dependence of sputtering yield.
Evolution of M26 is governed by:
  Material microstructure (post test statistics are insensitive to pre-test statistics)
  Differences in sputtering yield between components
a)
b)
depth z µm
Simulated normal-incidence domain with randomly distributed BN flakes:
a) Material (black BN, grey silica) b) Height-map for ~12 µm avg erosion depth

## Slide 37: Summary

## Slide 38: Conclusions
Plasma erosion of different materials governed by different mechanisms:
  Fused silica: Initial surface roughness propagates according to angle-dependent yield, but interesting microstructural patterns can result from initial surface roughness.
  M26 borosil: This complex material requires a more complicated model to describe erosion than a simple heterogeneous yield model.
  3D raytracing model for the erosion of heterogeneous materials can reproduce behavior of borosil erosion.
Stressed Erosion Experiment investigated the dependence of plasma erosion on applied mechanical stress.
  Result: No apparent differences between loaded and control samples are observed.
    For stresses of up to 25 MPa (cracking at 30 MPa)
    For temperature ranges of 200-300 C.
  Fused silica: Amplification functions were similar to within 0.05 (nondimensional)
  M26 borosil: Post-test surface statistics are similar to within 0.01 µm/wavemode.

## Slide 39: Conclusions
Thank you for your attention!
Questions?

## Slide 40: References
Garnier, Y., V. Viel, J. F. Roussel, D. Pagnon, L. Mange, and M. Touzeau. “Investigation of Xenon Ion Sputtering of One Ceramic Material Used in SPT Discharge Chamber.” In 26th International Electric Propulsion Conference, 512–17, 1999.
Satonik, Alexander J., and Joshua L. Rovey. “Modification of Boron Nitride Ceramic to Replicate Hall Effect Thruster Surface Wear.” AIAA-2012-0198, 50th Aerospace Sciences Meeting, Nashville, TN, 2012.
De Grys, K. H., Alex Mathers, Ben Welander, and Vadim Khayms. “Demonstration of 10,400 Hours of Operation on 4.5 kW Qualification Model Hall Thruster.” AIAA Paper 6698 (2010): 2010.
Schinder, Aaron, Mitchell Walker, and Julian Rimoli. “3D Model for Erosion of a Hall Effect Thruster Discharge Channel Wall.” Journal of Propulsion and Power, 2014. doi:10.2514/1.B35098.
Morozov, A. I. “The Conceptual Development of Stationary Plasma Thrusters.” Plasma Physics Reports 29, no. 3 (2003): 235–50.
Yim, John Tamin. Computational Modeling of Hall Thruster Channel Wall Erosion. ProQuest, 2008.
Gamero-Castano, Manuel, and I. Katz. Estimation of Hall Thruster Erosion Using HPHall. Pasadena, CA: Jet Propulsion Laboratory, National Aeronautics and Space Administration, 2005.
Yalin, A. P., B. Rubin, S. R. Domingue, Z. Glueckert, and J. D. Williams. “Differential Sputter Yields of Boron Nitride, Quartz, and Kapton Due to Low Energy Xe+ Bombardment.” AIAA Paper 5314 (2007).
R. A. Martinez, H. Dao and M. L. R. Walker, "Power Deposition into the Discharge Channel of a Hall Effect Thruster," Journal of Propulsion and Power, vol. 30, no. 1, pp. 209-220, 2013.
S. Mazouffre, J. P. Luna, D. Gawron, M. Dudeck and P. Echegut, "An infrared thermography study on the thermal load experienced by a high power Hall thruster," in 29th International Electric Propulsion Conference, Princeton, NJ, 2005.
Kim, K-S, JA Hurtado, and H Tan. “Evolution of a Surface-Roughness Spectrum Caused by Stress in Nanometer-Scale Chemical Etching.” Physical Review Letters 83, no. 19 (1999): 3872.