## Slide 1: Plasma Erosion of Stressed Fused Silica and M26 Borosil
Aaron M. Schinder
Advisor: Prof Mitchell Walker
Advisor: Prof Julian Rimoli
Georgia Institute of Technology
52nd AIAA/SAE/ASEE Joint Propulsion Conference
Salt Palace Convention Center, Salt Lake City, Utah
26 July 2016
Notes: I had 18 slides last time. I have 30 minutes: Perhaps 15 for the presentation and 10ish for questions.

## Slide 2: Overview
Motivation and Background
Stressed Erosion Experiment
Results of Fused Silica Exposures
Results of M26 Borosil Exposures
Modeling of Fused Silica Surface Evolution
Discussion of M26 Evolution
Conclusions

## Slide 3: Motivation and Background
Hall Effect Thrusters (HETs): Promising spacecraft propulsion technology for primary propulsion and station-keeping.
  High thrust to power.
  No space charge density thrust/area limitations.
HET lifetime limited by erosion of channel wall.
  Ions are created and accelerated.
  Some ions impact walls and sputter material.
  Walls erode over time, eventually exposing magnetic circuit.
  Considered end of life for the thruster.
Erosion process in HET channel wall: Ionization, acceleration region, erosion of discharge channel.
T-140 HET firing.

## Slide 4: Motivation and Background
Complex 3D structures are created during channel wall erosion.
Anomalous azimuthal ridges: Not explained by present models.
A more detailed understanding of plasma erosion is needed to understand the formation of these features.
  Interaction of plasma erosion with complex materials.
  Potential effects of thermo-mechanical stress in thrusters.
4
BPT-4000 after 10,400 hour life-testing, showing azimuthal erosion ridges. *
* de Grys. Mathers. Welander., “Demonstration of 10,400 Hours of Operation on a 4.5 kW Qualification Model Hall Thruster,” AIAA Joint Propulsion Conference, 2010-6698
SPT-100 after 5730-hr qualification life test
PPS-1350G after 2600-hr qualification life test

## Slide 5: Stressed Erosion Experiment
Test dependence of plasma erosion process on mechanical stress:
  Look into details of the evolution of surface features with and without mechanical load.
  Test samples exposed to argon plasma for 12 hours.
  Pairs of samples:
    Loaded: (Compressive stress up to 25 MPa).
    Control: Free to expand.
Material Selection:
  3x1x0.25 in samples: ~50mm region of >95% uniaxial stress.
  Fused Silica: Amorphous and isotropic. No microstructural detail.
  M26 borosil (60% BN, 40% SiO2 by mass): A composite material with complex microstructure.
3x1x0.25 in Fused Silica Sample with Attached Strain Gage
SEM Microscopy of M26 Borosil
1μm
Boron Nitride
Silica Grain
Further details in: Schinder, A., Rimoli, J., Walker, M. “Investigation of Plasma Material Erosion under Mechanical Stress,” Journal of Propulsion and Power, (Accepted July 2016).

## Slide 6: Test Fixture Design
Test Fixture Design:
Plasma
Preheater Pads
Experiment Sample
Control Sample
Strain Gages
Plasma Source
Thermocouple
16 cm
Top: IAD Chamber diagram showing test fixture positioned over plasma source.
Left: Test fixture in IAD chamber.
Plasma at normal incidence to samples, ~110 eV, 3mA/cm2 argon plasma.

## Slide 7: Test Procedure
Test Phases:
  Pre-exposure phase.
    Tencor P-15 Contact Profilometer: Collects surface line-scans.
    Olympus LEXT Confocal Microscope.
  Exposure phase.
    Samples loaded to desired load.
    Sample pairs exposed to argon plasma for 12 hrs.
  Post-exposure phase.
    Repeat the surface profilometry and microscopy.
    Fourier transformed surface line-scans provide surface statistics: Amplitude vs. spatial frequency of features.
    Amplification function Ψ:
      Ψ>0 Features growing.
      Ψ<0 Features damped.
Ψ
ω, or ν
ωcr
ωmg
Olympus LEXT 3D Microscope
Contact Profilometry Line-scan on Sample Surface
Amplification Function

## Slide 8: Results of Fused Silica Exposures
3 Pre-roughened fused silica exposures:
  11 hrs exposure to 120 eV argon plasma.
  Erosion depths of 20-40 µm
  3 load levels:(6.00±1.01, 14.36±1.01, 24.99±1.10 MPa)
  Each sample pair develops same Ψ to within 0.05
  No apparent dependence on applied load
  Growth of features larger than100 µm
  Damping of smaller features.
Amplification function (with 7-point spatial frequency average) as a function of spatial frequency.
Figure shows ratio of pre vs. post-test amplitude. Ψ>0 shows spatial frequencies that are growing.
Control and loaded samples have same growth function

## Slide 9: Results of Fused Silica Exposures
a,b) Pre-test microscopy laser height-map and optical image, c,d) Post-test microscopy laser height-map and optical image

## Slide 10: Results of Fused Silica Exposures
Sample SA9: Smooth (no pre-roughening). One area scored by stylus.
  Initially smooth areas remain smooth.
  Scratched areas develop cell pattern.
Laser image of Sample SA9 scratch mark a) Pre-exposure, b) Post-exposure

## Slide 11: Results of M26 Exposures
Two exposures with M26 borosil conducted.
  12 hrs exposure to 120 eV argon plasma.
  Erosion depths:12.5 ± 2.5 µm
  Load levels: (20.6±3.3 MPa, 24.1± 3.4 Mpa).
  Pre-test surface roughness statistics vary by 0.1 µm/wavemode.
  Post-test roughness same to within 0.01 µm/wavemode.
  No dependence on the applied load is apparent.
Pre vs. post-exposure averaged Fourier transformed surface amplitude as a function of spatial frequency (surface roughness statistics) for M26.
Control and loaded samples have same post-exposure statistics

## Slide 12: Results of M26 Exposures
SC3 (control), 20x, Pre-exposure surface a) visual image, b) surface height profile, Post-test surface c) visual image, and d) surface height profile.

## Slide 13: Results of M26 Exposures
c)
M26 Sample SC1 100x image:
Optical image, b) Laser height-map
c) LEXT 3d visible image overlaid on height-map

## Slide 14: Modeling of Fused Silica Cell Development
Cusped cell pattern explained by fused silica sputtering yield angle dependence:
A simple 1D model, taking into account local ion impact angle:
  Reproduces formation of cusps.
  Reproduces qualitative and quantitative post-exposure profiles.
Relative yield as a function of ion impact angle. Data from Yalin *.
Right: Experimental surface profiles (blue). Pre-exposure and post-exposure profile from SA5.
Black lines propagate the pre-exposure surface profile according to the model.
*Yalin, A. P., Rubin, B., Domingue, S. R., Glueckert, Z., Williams, J. D., " Differential Sputter Yields of Boron Nitride, Quartz, and Kapton Due to Low Energy Xe+ Bombardment," AIAA Paper 5314-2007, American Institute of Aeronautics and Astronautics, 2007.

## Slide 15: Modeling of Fused Silica Cell Development
Comparison of statistics from 50 simulated line-scans to experimental pre vs. post-test statistics:
Amplification function Ψ as a function of spatial frequency for experimental and simulated profiles.

## Slide 16: Discussion of M26 Evolution
Evolution of M26 is independent of pre-exposure statistics/roughness.
  Dominated by complex material microstructure.
  Boron nitride flakes have lower yield than fused silica matrix.
  BN Flakes protrude from surface.
3D raytracing model of surface evolution. *
  Models complex heterogeneous material domain.
  Reproduced development of surface features seen on AFRL/UM P5.
  Reproduced cliff-and-valley structures in eroded channel wall.
* A. Schinder, M. Walker, and J. Rimoli, “3D Model for Erosion of a Hall Effect Thruster Discharge Channel Wall,” Journal of Propulsion and Power, vol. 30, no. 5, pp. 1373–1382, 2014.
16
a)
b)
depth z µm
Simulated normal-incidence domain with randomly distributed BN flakes:
a) Material (black BN, grey silica) b) Height-map for ~12 µm avg erosion depth

## Slide 17: Conclusions
Fused silica surface development governed by:
  Pre-exposure surface profile (pre-exposure surface statistics proportional to post-exposure statistics).
  Angle dependence of sputtering yield.
Fused silica develops interesting cusped-cell pattern from a pre-roughened surface.
M26 surface development governed by:
  Material microstructure.
  Difference between sputtering yield of BN flakes and silica matrix.
  Post-exposure statistics are independent of pre-exposure statistics.
  Unlike for fused silica, M26 microstructure dominates any influence of 1.55±0.10 µm rms pre-existing surface roughness.
No apparent dependence of plasma evolution of surfaces on mechanical stress found. (For stresses of up to 25 MPa, for fused silica and M26).
  Fused silica amplification functions are the same to within 0.05.
  M26 post-exposure statistics are the same to within 0.01 µm/wavemode.

## Slide 18: Acknowledgements
This work was funded by a National Defense Scientific and Engineering Graduate (NDSEG) fellowship, and by the Air Force Office of Scientific Research (AFOSR) under grant number FA9550-11-1-0160. The authors would like to thank the American Society for Engineering Education (ASEE) and AFOSR for supporting this research. In addition, the authors would like to thank Dr. Jud Ready and Dr. Brent Wagner of the Georgia Tech Research Institute for the use of their chamber and plasma source. The authors would like to thank Thomas Burton and Professor Gregory B. Thompson of the University of Alabama for their help conducting SEM microscopy of the AFRL/UM P5 channel wall.

## Slide 19: Thank You
Questions?